| TYPICAL DATA SHEET Revised 8/1/02 | CMP-4001 Hydro-Fused(/Compressed MicroPore Gasket Material |
| --- | --- |

DESCRIPTION:

A high performance, Compressed MicroPore material, produced with our exclusive Hydro-Fused( production process. It is a unique binder blend and synthetic fiber matrix. It has excellent sealability and torque retention properties and is recommended for OEM and industrial applications. For use in applications with intermittent operating temperatures up to 288oC (550oF). CMP-4001 conforms to: Mil G 24696 SH(B)

| TYPICAL DATA: |  |
| --- | --- |
| Material Gauge | 0.8 mm |
| Density g/cm3 (lbs./cu. ft.) | 1.60 (100) |
| Compressibility % at 34.5 MPa (5000 psi) | 10 |
| Recovery (%) | 64 |
| Tensile - MPa (psi) - Cross Direction - Machine Direction | 23 (3300) 32 (4600) |
| ASTM F-146 IMMERSION TESTING IRM 903 - 5 hours at 150oC (300oF) |  |
| Percent Change in Thickness | 5 |
| Percent Change in Weight | 9 |
| Percent Change in Tensile Strength | -12 |
| Fuel B - 5 hours at 21-24oC (70-75oF) |  |
| Percent Change in Thickness | 12 |
| Percent Change in Weight | 12 |
| Glycol/Water 50/50 - 5 hours at B.P. |  |
| Percent Change in Thickness | 3 |
| Percent Change in Weight | 10 |
| Oil #1 - 5 hours at 150 C (300 F) |  |
| Percent Change in Thickness | 1 |
| Fuel C - 5 hours at 21-24oC (70-75oF) |  |
| Percent Change in Thickness | 13 |
| Percent Change in Weight | 12 |
| Creep Relaxation - 22 hours, 100 C (ASTM F38B) | 17 |
| Sealability - Fuel A (ASTM F37A) | 0.0 |
| Color | Natural |

REMARKS:

Hydro-Fused, Pro-Formance, Syntheseal, Thermo-Tork and Accoseal are trademarks of Interface Solutions, Inc. Select-a-Seal is a registered trademark of Interface Solutions, Inc.

| Please understand that you are responsible for the accuracy of all project specifications; including any Interface Solution guide specifications that you use. INTERFACE SOLUTIONS SHALL NOT BE LIABLE FOR ANY DAMAGES ARISING OUT OF THE USE OF ANY OF ITS GUIDE SPECIFICATIONS. |  |
| --- | --- |

WWW.SEALINFO.COM